| EPX 80W-90 |  |
| --- | --- |
|  | 20.08.2003 |

DESCRIPTION

Castrol EPX 80W-90 is a mineral based, extreme pressure multi-purpose gear oil

designed for the lubrication of spiral bevel, hypoid differentials and manual

transmissions where the manufacturer recommends the use of an oil to API GL5

performance level.

This product is formulated from high quality mineral base stocks and contains

a selection of additives which impart extreme pressure, anti-corrosion,

anti-oxidant and anti-foam properties

APPLICATION

Castrol EPX 80W-90 provides excellent protection to gears operating under the

most severe service conditions.  The multigrade viscosity permits its use over a

wide range of operating temperatures, being particularly effective at low

temperatures.

FEATURES/BENEFITS

Superior anti-wear performance

Good thermal stability and resistance to oxidation

Reduced wear

Product rationalisation

PERFORMANCE

API Service Level 	GL5

US Claims	MIL-L-2105D - Meets Requirements

ZF TE-ML-	01A/05A/07A/12A - Approved

TYPICAL CHARACTERISTICS

SAE Viscosity Rating	80W/90

Relative Density @ 20º C	0.895

Viscosity @  40º C, mm²/s	133.7

Viscosity @ 100º C, mm²/s	14.0

Viscosity Index	101

Flash Point (closed) º C	173

Pour Point   º C	-30