| GTX 3 Magnatec 10W-40 |  |
| --- | --- |
|  | 24.04.2002 |

DESCRIPTION

Modern engines need a different type of oil from conventional engines.

New Castrol GTX 3 Magnatec has been synthetically

engineered to provide enhanced protection for this specific use.

Every time you start your car it takes a while for your engine to get effective

protection from an ordinary oil, because the oil cannot protect properly until it

reaches a critical temperature - as a result independent tests show up to 75% of

engine wear occurs in the first ten minutes.

Castrol GTX 3 Magnatec is different as it gets to work straight away by virtue

of a unique synthetic ester that clings to engine surfaces like a magnet - this “Unique Molecular

Attraction” provides up to 4 times more protection than a conventional oil during the

critical start and warm up period

APPLICATION

10W-40 viscosity oils are widely recommended for a variety of engines manufactured since 1990.

FEATURES AND BENEFITS

New Castrol GTX Magnatec offers 4 times better wear protection than ordinary oils

More than 3 times better at reducing engine wear than current Castrol GTX Magnatec

Up to 60% better than the competitor grades we compared Castrol GTX Magnatec against

Unique triple layer formula with active molecules clinging to engine parts

PERFORMANCE

API	SL/CF

ACEA	A3/B3

VW	500 00/505 00 (meets requirements)

TYPICAL CHARACTERISTICS

Appearance	Bright, clear liquid

SAE Viscosity Rating	10W-40

Density at 20°C, g/cm³	0.887

Viscosity at 40°C, mm²/s	109.3

Viscosity at 100°C, mm²/s	15.4

Viscosity Index	148

Pour Point, °C	-27

Closed flash point ºC	195

TBN	10.4