| Response DOT 4 |  |
| --- | --- |
|  | 03.09.2001 |

DESCRIPTION

Castrol Response DOT 4 is a high performance, synthetic brake fluid which exceeds the requirements of the SAE J1703, FMVSS116 DOT 3 and DOT 4, ISO 4925 and JIS K2233 specifications.

Castrol Response DOT 4 Brake Fluid is formulated from mixed polyalkylene glycol ethers and borate esters, together with carefully selected additives. These enable the fluid to operate at a high performance level throughout its service life, offering system protection together with ultimate braking confidence.

APPLICATION

Castrol Response DOT 4 Brake Fluid is especially formulated to meet the demanding requirements of modern, high performance, automotive brake and clutch systems with the exception of those for which a mineral oil based fluid is specified (for example, some Citröen systems, for which Castrol LHM is suitable and Rolls Royce systems, for which Castrol HSMO Plus is approved).

As with all brake fluids which contain glycol ethers, care should be taken to avoid spilling this product on paintwork as it may have a damaging effect. In case of spillage, rinse the affected area with water immediately: Do not wipe.

It is fully compatible with other fluids meeting FMVSS 116 DOT 3, DOT 4 and DOT 5.1 however, in order to maintain the superior performance characteristics of Castrol Response DOT 4, avoid mixing with other brake fluid products.

All conventional brake fluids deteriorate during use. It is strongly recommended that Castrol Response DOT 4, should be changed according to the vehicle manufacturers advice. In the absence of such advice, a 2 year change period is recommended.

PERFORMANCE

SAE J1703

FMVSS 116 DOT 4

TYPICAL CHARACTERISTICS

Dry Boiling Point ºC	270

Wet Boiling Point ºC	ca 170

Viscosity at -40ºC mm²/s	1200

Viscosity at 100ºC mm²/s	2.3

pH	7.7