| TQ-D |  |
| --- | --- |
|  | 18.07.2003 |

DESCRIPTION

Castrol TQ-D is an automatic transmission fluid designed specially to meet the requirements of the former General Motors Dexron®

II D specification.

APPLICATION

.Castrol TQ-D fully  meets the requirements of Dexron® II D type fluid and is suitable for all transmissions calling for this level of specification. TQ-D is recommended for use in the automatic transmissions and power steering fitted to many other types of vehicle, including later Fords where fluid to ESP-M2C166-H or SQM-2C9010-A is specified. Also for semi-automatic transmissions where a Leyland spec E fluid is specified.

FEATURES/BENEFITS

Good oxidation resistance

Excellent frictional characteristics

Extended drain potential

Reduced wear

More efficient operation

PERFORMANCE

FORD ESP-M2C166-H	Meets requirements

FORD SQM-2C9010-A	Meets requirements

ALLISON C-4 	Meets requirements

MB 236.6	Approved

ZF TE-ML 02F/03/04D/11A/14A 	Approved

| All reasonable care has been taken to ensure that the information contained in this publication is accurate as at the date of printing. It should be noted however that the information above may be affected by changes occurring subsequent to the date of printing in the blend formulation or methods of application of any of the products referred to or in the requirements of any specification approval relating to any such products. | 1 of 2 |
| --- | --- |

| TQ-D |  |
| --- | --- |

TYPICAL  CHARACTERISTICS

Relative Density  @  20oC			0.870

Viscosity @ 40ºC, mm²/s 			33.0

Viscosity  @  100oC, mm²/s.			7.1

Brookfield Viscosity @ -40o  cP max. 	50,000

Viscosity Index min.				165

Pour Point  oC  max.				-39

Flash Point (open)  oC  min.	 		186

FOAM TEST (mls) TYPICAL VALUE :		TENDENCY		STABILITY

@  23.9oC						     	10			0

@  93.3oC							40			0

@  23.9oC  after 93.3oC					10			0