| Transmax Z |  |
| --- | --- |
|  | 26.11.2001 |

DESCRIPTION

Castrol Transmax Z is a fully synthetic automatic transmission fluid which also has use in manual transmissions.

APPLICATION

Castrol Transmax Z is recommended for all buses and coaches fitted with automatic and semi-automatic transmissions and may also be used in manual transmissions.  As such it is recommended for fleets employing a mixture of Voith, Renk, ZF, Allison and MB transmissions alongside the Leyland Pneumocyclic and Hydracyclic units.

Extended oil drain [90.000 km] in ZF Ecomat MB AT and Voith AT.

FEATURES/BENEFITS

Excellent thermal and oxidative stability giving cleanliness reducing servicing and giving extended drain performance

Excellent temperature reduction through reduced friction giving reduced emissions and fuel economy

Optimised frictional characteristics providing smoother gear changes and much less wear

Outstanding cold flow properties giving high protection to transmission especially at start-up

Unique shear stability properties - constant viscosity during oil life

Excellent anti-foam behaviour

Good extreme pressure and anti-wear performance for longer transmission life

Very good seal performance reducing oil leakages

Free from chlorine and heavy metals for reduced environmental impact

| All reasonable care has been taken to ensure that the information contained in this publication is accurate as at the date of printing. It should be noted however that the information above may be affected by changes occurring subsequent to the date of printing in the blend formulation or methods of application of any of the products referred to or in the requirements of any specification approval relating to any such products. | 1 of 2 |
| --- | --- |

| Transmax Z |  |
| --- | --- |

PERFORMANCE

API GL3/GL4

ZF TE-ML- 02F/ 03/ 09B/11B/14C 	Approved

MB 236.81 	Approved

MAN 339C	Approved

Renk	Approved

Voith - G607/ G1363 	Approved

ZF 8S-180 manual bus transmission	Approved

TYPICAL CHARACTERISTICS

SAE	70W-80

Density @ 15ºC	0.836

Viscosity @ 40ºC	38

Viscosity @ 100ºC	7.5

Viscosity Index	169

Pour Point ºC	<-60

Flash Point º	228